## Slide 1: GeO2 simualtions & target design
Tommaso Vinci
ESRF January 19, 2016

## Slide 2: Target Design
CH 5µm
Al 30µm
GeO2 15µm
LiF 150µm
CH
5µm
Al
30µm
GeO2
15µm
LiF
150µm
0
150
165
195
200
µm

## Slide 3: Target Design : ablator
CH 5µm ablated material over 10ns
Al 30µm
GeO2 15µm
LiF 150µm
CH
5µm
Al
30µm
GeO2
15µm
LiF
150µm
0
150
165
195
200
µm

## Slide 4: Target Design : shield
CH
5µm
Al
30µm
GeO2
15µm
LiF
150µm
CH 5µm ablated material over 10ns
Al 30µm to prevent X-rays preheat
GeO2 15µm
LiF 150µm

## Slide 5: Target Design : Germanium
CH
5µm
Al
30µm
GeO2
15µm
LiF
150µm
CH 5µm ablated material over 10ns
Al 30µm to prevent X-rays preheat
GeO2 15µm by the k edge absorption
LiF 150µm

## Slide 6: Target Design : LiF
CH
5µm
Al
30µm
GeO2
15µm
LiF
150µm
CH 5µm ablated material over 10ns
Al 30µm to prevent X-rays preheat
GeO2 15µm by the k edge absorption
LiF 150µm by feasability / price / x-ray absorption

## Slide 7: Simulations: top view
Laser ω 2x1013 9ns
Visar
LiF
GeO2
Al
CH
~15km/s

## Slide 8: Simulations: intensity scan
0.2x1013W/cm2
0.5x1013W/cm2
1.0x1013W/cm2
2.0x1013W/cm2
~15km/s
~12km/s
~8km/s
~10km/s

## Slide 9: Simulations: pressure and temperature
0.5 ns
Temperature [1000K]
Pressure [Mbar]
0.2 - 0.5 - 1.0 - 2.0 x 1013 W/cm2

## Slide 10: Phase diagram
2x1013
1x1013
5x1012
2x1012

## Slide 11: Ramp compression

## Slide 12: Ramp compression

## Slide 13: Ramp compression